PMC-C-Green-40

Hollow-Core Fiber optimized for green spectral range.

- Nearly single mode guidance

- Low dispersion, low loss

- High power and energy handling

| Physical Properties |  |
| --- | --- |
| Core contour | Hypocycloïd |
| Inner core diameter | 40 µm ± 2µm |
| Outer fiber diameter | 230 µm ± 1% |
| Fiber coating diameter | 400 µm ± 30µm |
| Optical Properties |  |
| Attenuation @ 515 nm | <30 dB/km |
| Attenuation @ 532 nm | <30 dB/km |
| Dispersion @ 532 nm | 1 ps/nm.km ± 0.5 |
| Mode Field Diameter (1/e²) @ 532nm | 26 µm ± 1 µm |
| M² @ 532nm | <1,2 |
| N.A. | 0.014 ± 0.002 |

Broad spectral coverage

Typical attenuation and dispersion

Output near field profile

Output far field profile

All specifications may be changed without notice

123 avenue Albert Thomas - 87060 Limoges Cedex France

www.glophotonics.fr

contact@glophotonics.fr